## Slide 1: Physical and Chemical Analysis of Dredging Material from the Dead Sea Environment
Khatri, Madhav
Final Presentation for Study Project
Supervisor :Prof. Dr.-Ing. Bernhard Vowinckel
A student of M.Sc. Hydro Science and Engineering
Dresden, 30.01.2024

## Slide 2
Introduction: Brief context of the study
Fig 1: Location of the Dead Sea
Picture extracted from (N. G. Lensky et al., 2005)
Source: Google map
Fig 2: A closer view of the study area
Evaporation ponds for salt extraction

## Slide 3
Introduction: A brief context of the study
About 20 million tonnes of salt precipitate each year, creating a layer of approximately 20 centimeters at the bottom of the evaporation ponds.
(Salt Harvesting - ICL, 2023)
Reznik and Gavrieli (2023)
Figure 3: A closer look on the dredging activities

## Slide 4
Introduction: A brief context of the study
Nahal Arava
Fig4: Google earth picture representing Nahal Arava with dotted red line
Source: Google earth

## Slide 5: Research Questions
Can the accumulated salt be dumped into the Nahal Arava river and transported to the Dead sea as a granular material?
Objectives:
To study the physical properties- sieve analysis, density, turbidity
and chemical properties- elemental composition, solubility of the salt sample

## Slide 6: Results: Sieve analysis
Fig: 5(b) Sample Divider
Fig: 5(a) Air dried sample
Fig: 5(c) Standard Sieve Sizes
Plot 1: Plot of sieve analysis curve for two runs

## Slide 7: Results: Sieve Analysis
D50 is the key term that enters in Meyer Peter Müller formula
Plot2: Combined sieve analysis
Median salt size | 1800 microns
(Analysensiebe, Blau-Metall, 2023)

## Slide 8: Results: Experiment on solubility
One litre of distilled water can dissolve approximately 300 grams to 350 grams of halite until it becomes saturated
Gradual addition of salt sample to raw water (500mL) at 21.5 degrees at constant stirring of 600 rpm with magnetic stirrer |  |  |  |  |  |  | 
Initial water taken = 500 ml |  |  |  |  |  |  | 
Density(g/L) | Left over crystals? | T(°C) | EC(mS/cm) | Salt(g) | Time salt is fully dissolved | Cumulative salt(g) | Remarks
0.9464 | no | 21.5 | 1 | 0 | 0 | 0 | 
0.9946 | no | 21.3 | 70.7 | 25 | 165 | 25 | 
1.045 | no | 20.7 | 122.4 | 25 | 236 | 50 | 
1.0942 | no | 21 | 162.3 | 25 | 521 | 75 | 
1.1418 | no | 21.1 | 193.3 | 25 | 888 | 100 | 
1.1914 | no | 21.4 | 216 | 25 | 984 | 125 | 
1.2396 | very small | 22.4 | 231 | 25 | 1219 | 150 | Saturation Point
1.2882 | Yes, clearly insoluble | 22.6 | 239 | 25 | 1320 | 175 | 
Solubility of salt sample = 300g/L- 350 g/L |  |  |  |  |  |  | 
Table1: Table for solubility test

## Slide 9: Results:
https://www.worldatlas.com/articles/the-world-s-most-saline-bodies-of-water.html
Saline conditions are similar to solubility of salt sample

## Slide 10: Results- Behaviour of density and Electroconductivity(EC) with salt addition
Plot3: Density, EC vs salt addition

## Slide 11: Results: Settling Velocity in brine condition
 | weight of vessel(g) | Volume(ml) | weight of vessel including salt(g) | Bulk Density(kg/m3)
sample 1 | 103.05 | 200 | 356.85 | 1269
sample 2 | 104.05 | 150 | 297.85 | 1292
sample 3 | 77.85 | 500 | 670.4 | 1185.1
 |  |  | Bulk density | 1248.7
(Weisbrod et al., 2016)
(From lab)
Plot 4: settling velocities of salt particles under brine condition
Table2: calculations for bulk density of salt sample

## Slide 12: Results-Particle Count Analysis
Plot5(a): Plot of particle size vs. Number of particles
Plot5(b): CDF Plot of particle size
Fig5: salt solution displaying turbidity
particulate substances that are not dissolved in the solution
Size belonging to Clay and silt fraction
Particle size analysis was conducted on the residues remaining after the dissolution experiments of salts
Fig6: classification schemes to define ranges of grain diameters for clay, silt, sand, and gravel.

## Slide 13: Results-ICP- MS (Inductively Coupled Plasma- Mass Spectrometry)
Presence of trace elements like Fe and Al
Plot6(b): Composition of halite
Plot6(a) : Composition of elements except Sodium in halite

## Slide 14: Conclusions:
Salt particle size in the range- 250 microns to 4000 microns with median size 1800 microns
Calculated Bulk density of salt~1250 kg/m3
Salt grains are equivalent to coarse sand-fine gravel
Composition: Sodium-98.90 % Other elements- 1.1%, detection of trace elements like Fe, Mg and Al
The diluted salt solution was found turbid-indicating presence of particulate substances that are not dissolved in the solution. So, because of its dirty nature and detection of elements like Fe, Al, it becomes expensive to make use of accumulated salt(approximately 20 million cubic meters of salt annually).
Solubility of the salt was found approximately equal to the salinity of water in the dead sea region.
Under brine conditions, the halite settles down in the river

## Slide 15: Outlook:
The real brine solution from the river could be taken and studied out to see and observe more real scenarios
Knowledge of proper flow conditions of the Nahal Arava would help calculate more scientifically the transportation feasibility of salt sample as a granular material

## Slide 16
Thank you!
Any questions?